Code 01: Non-protective packaging for plates (export)

(Available on enquiry only)

###### Specifications

|  | Plate mill |
| --- | --- |
| Local | L ( 15000mm |
| Export | L ( 12000mm |
| Rail | W ( 2400mm |
| Road | W ( 3200mm |
| Wall Height | 350mm |
| Lift mass | Bundles: 13T Max. export |

Strapping

| Plate Length (mm) | No of straps |
| --- | --- |
| L < 6000mm | 3 |
| 6000 ( L< 8000mm | 4 |
| L ≥ 8000mm | 5 |

Additional notes:

i.	Bundle mass = lift mass = packing mass ( max. handling mass

ii.	For orders with bundle mass < 5T, refer to Code 10 for overlap if handling

capacity requires this.

## Corrosion considerations

Packaging classified as non-protective provides no protection against corrosion, accordingly the material will be susceptible to corrosion under wet and humid conditions.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |
| --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Steel plates | MP, MPSQ, MPLQ, MPG | 110/111 | 0 | n/a | n/a | n/a |

* Days after receipt of material.

n/a- not available.

Note:

Depending on the prevailing weather conditions and precautions taken during transit, the material may

corrode as no protection is provided by this packaging method.

# Text boxes

Packaging specification: 01

Non-Protective Packaging for Plate

Loose and bare with straps

- Labels - centre, opposite edges - top surface

- Die stamp marks

- Stencil mark

- Harbour colour marks

- Straps

- Wood

- Lift