Code 08: Non-protective packaging for Cold Rolled & Galvanised (local) and Secondary (all) Coils

- 3 Circumferential straps

- 3 Eye ties

- Eye ring

- Seal

- Outer Corner Bracket

I.    Information label

Note:

A seal protector will be placed underneath the seal of the centre circumferential strap.

Corrosion considerations

Packaging classified as non-protective provides no protection against corrosion, accordingly the material will be susceptible to corrosion under wet and humid conditions.

| Description | Product Code | SPE | * Allowed claim period per surface treatment |
| --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Cold Rolled/Drawing & Forming coils | CC, CCH | 130 | 0 | n/a | n/a | 0 |
| Galvanized Coils | GC | 140 | 0 | 0 | n/a | 0 |

* Days after receipt of material.

n/a- not available.

Note:

Depending on the prevailing weather conditions and precautions taken during transit, the material may

corrode prematurely as no protection is provided by this packaging method.

# Text boxes

Packaging specification: 08

Non-protective Packaging with Eye Ties, Circumferential Straps and Eye Ring