Packaging specification: 09

Vertically Packed Non-Protective Packing with Eye Ties, Masonite, Circumferential Straps and Eye Ring

Code 09: Non-protective packaging

- Circumferential strap applied over Masonite

- 4 Eye ties

- Eye ring

- Seal (applied on top of Masonite circumferential protection)

- For roofing products: 2 x 250mm masonite strips on circumference

For appliance white:

<925mm   = 2 strips

≤1200mm = 3 strips

>1200mm = 4 strips

6.	Outer corner bracket

7.	Plastic

8.	Standard wooden pallet

I.   Information label

## Corrosion considerations

- Packaging classified as non-protective provides no protection against corrosion, accordingly the material could be susceptible to corrosion under wet and humid conditions.

- The plastic is not protected and could tear during normal handling operations. The likelihood of premature surface deterioration will be enlarged.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Textradek® , Galv, Chromadek®,Chromaprep® | DGC, KGC, PGC | 145/146/147 | 0 | n/a | n/a | 0 |

* Days after receipt of material.

n/a- not available.

Note:

Depending on the prevailing weather conditions and precautions taken during transit, the material may corrode prematurely as no protection is provided by this packaging method.