Code 32: Advanced protective packaging for Vanderbijlpark colour coated coils

(Export)

- Strapping 0,9 x 32mm	     8.  	Eye tie

- Outer corner bracket  	     9.  	Wooden pallet

- Seal	    10.  	Wooden block

- Eye ring	    11.  	Shore wood

- Top hat	    12.  	2 X 300 mm masonite strip on circumference

- Eye plate	     I.   	Information label

- Cover sheet

Specification

Store in CM 4 at Works. Max stacking height = 4. Transport by road only.

Corrosion considerations

- Packaging classified as Advanced Protective has masonite strip on circumference and cover sheet.

- Although advanced, the packaging is not fully airtight which implies that coils must be appropriately protected against rain and wetness during loading, transit and off-loading.

- To prevent condensation and premature deterioration of strip surface condition, the coils must be stored in a dry, ventilated warehouse.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |
| --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Textradek® CR/Textradek® Galv, Chromadek® , Chromaprep® | DCC, DGC, KGC, PGC | 135/145 | 120 | n/a | n/a | n/a |

* Days after receipt of material.

n/a- not available/applicable

Note:

- Claims for corrosion will only be considered by Mittal Steel South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above,

- Once protective packaging has been removed and material taken into stock, Mittal Steel South Africa will not consider any claims for corrosion.

# Text boxes

Packaging specification: 32

Advanced Protective, Vertically packed Packaging for Sensitive Material