Code 64: Advanced protective packaging for

Electro-galvanized and Cold Rolled ISF coils (local)

- Circumferential strap (no centre circumferential strap on ISF)

- Reinforced PE VCI Paper

- Two Masonite strips (one each side) 3.5 m max

- Outer corner bracket

- Edge protection (outer corner)

- Top hat	I. 	Information label

- Eye ring	A.	Unwinding direction sticker

- Eye plate with Inner Masonite Strip	D.	Handling label (see annexure C)

- 5 Eye ties

- Seal

- Cover sheet

- Moisture indicator (2 stickers per coil, on both ends)

Specifications

1.   No centre circumferential strap underneath the packing material.

2.   Only 2 circumferential straps on outer corner brackets if ISF material.

Corrosion considerations

- Packaging classified as Advanced Protective has corrosion protection provided by covering the material with plastic together with a galvanized cover sheet.

- The packaging is not fully airtight which implies that the coils must be appropriately protected against rain and wetness during loading, transit and off-loading.

- To prevent condensation and premature deterioration of strip surface condition, the coils must be stored in a dry, ventilated warehouse.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |
| --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| Cold rolled/ drawing & forming coils | CCI | 131 | 0/30@ | n/a | n/a | 90 |
| Zincrometal coils | SCC | 136 | 90 | n/a | n/a | 60# |
| Electro-galvanised coils | EC, ECI | 148 | 0/30* | n/a | n/a | 90 |

* Days after receipt of material.

n/a- not available/applicable

Note:

- @ 0 days guarantee given for dry material, 30 days applicable to material treated with aqueous skin passing rust preventative fluid.

- # The 90 days on Zincrometal applicable to material that is not oiled and coated on both sides. compared to the 60 days for material that is oiled but coated only on one side.

- Claims for corrosion will only be considered by Mittal Steel South Africa if the material has been properly stored in a dry, ventilated warehouse, and the claims submitted within the periods indicated above.

- Once protective packaging has been removed and material taken into stock, Mittal Steel South Africa will not consider any claims for corrosion.

- * 0 days guarantee given for dry material in coastal / high humidity conditions. 30 days applicable to inland / dry conditions.

# Text boxes

Packaging specification: 64

Advanced Protective Packaging with Reinforced, PE-Coated VCI Paper, Cover Sheet, Eye Ring and Edge Protection