Code 94: Non-protective packaging for

Hot rolled coils 1,6 mm to 2,5 mm

- Angle Bracket (32 mm X 0.9 mm)

- One Hilty Nail per side on Inside Wrap, 10 mm from Strip Edge, near Strip End (Hilty Nail: 14.5 x 1.45 mm)

- Circumferential Straps (32 mm X 0.9 mm)

I.   Information Label

Specifications

See table 1 for number of circumferential straps.

Strapping specification

Table 1: number of circumferential straps and eye straps required

| Thickness (mm) | Width (mm) |
| --- | --- |
|  | < 1000 | 1000 - 1500 | > 1500 |
| 1,6 – 2,5 | 3 circumferential | 4 circumferential | 5 circumferential |

Corrosion considerations

Packaging classified as Non Protective provides no protection against corrosion, accordingly the material will be susceptible to corrosion under wet and humid conditions.

Corrosion guarantee

| Description | Product code | SPE | * Allowed claim period per surface treatment |
| --- | --- | --- | --- |
|  |  |  | None | Passivated | Dos oil | Rust preventative oil |
| HR Coils | HC HCW | 120 | 0 | n/a | n/a | 0 |

* Days after receipt of material.

n/a- not available/applicable.

Note:

Depending on the prevailing weather conditions and precautions taken during transit, the material may corrode prematurely as no protection is provided by this packaging method.

# Text boxes

Packaging specification: 94

Non-Protective Packaging with Circumferential Straps and Two Hilty Nails on Inside Wrap